|  | PT-**-H (Low Residual) |
| --- | --- |
| 主要適用對象 Application | security bag |
| 基材 Base material | 霧面聚脂膜(PET) Mist PET Film 厚度0.04mm Thickness 0.04mm |
| 底紙 Base paper | PET 離型膜25μ silicone release film Thickness 0.025mm |
| 膠系 Adhesive type | 壓克力感壓膠 Acrylic Pressure Sensitive Adhesives |
| 總厚度 Total thickness | 0.07±0.01mm |
| 黏著 力 Holding power | g/25mm | ＞700 |
| 保持力 Holding Power for Temp. Resist | 40℃ | ＞48 hrs |
| 保存期限 Expiry date | 從製造日期起12個月內 Within 12 months from manufacturing date |
| 公版顯跡內容 Peel off text | OPEN VOID |
| 環測條件 Testing environment | 按JIS Z 0237 J.DOW Method 測試 21.1℃ x 51.55%R.H Test according to JIS Z 0237 J.DOW Method, 21.1℃ x 51.55%R.H |
| 有效顯跡溫度 Effective temperature | 無限制 無法破解 No boundary, non-hackable. |