|  | NT-**-H Non-Transfer (No Residual) |
| --- | --- |
| 主要適用對象 Application | Metal Baking varnish ABS molding plastic products Glass |
| 基材 Base material | 霧面聚脂膜(PET) Mist PET Film 厚度0.04mm Thickness 0.04mm |
| 底紙 Base paper | 格拉辛離型紙 Glassing silicone release paper Thickness 0.07mm 80g/㎡ |
| 膠系 Adhesive type | 壓克力感壓膠 Acrylic Pressure Sensitive Adhesives |
| 總厚度 Total thickness | 0.09±0.01mm |
| 黏著 力 Holding power | g/25mm | 800±200g |
| 保持力 Holding Power for Temp. Resist | 40℃ | ＞48 hrs |
| 保存期限 Expiry date | 從製造日期起12個月內 Within 12 months from manufacturing date |
| 公版顯跡內容 Peel off text | OPEN VOID |
| 環測條件 Testing environment | 按JIS Z 0237 J.DOW Method 測試 21.1℃ x 51.55%R.H Test according to JIS Z 0237 J.DOW Method, 21.1℃ x 51.55%R.H |
| 有效顯跡溫度 Effective temperature | (視被貼物不同 效果不同, 請自行測試,304不銹鋼板80℃以上) Adhesive works differently depends on the target surface. Please make test on your target surface. Our product works well on 304 stainless steel at 80 “ C |